SOURCE CONTROL SPECIFICATION

Part Number: C.SLQ003

Only the item described in this source control to meet the specification listed herein is approved by SILQ.  A substitute item shall not be used without prior approval.

# Purpose

## This document provides the specification for the 55 gallon plastic drum.

# Supplier

## Uline, 12575 Uline Drive Pleasant Prairie, WI 53158, Tel: 1-800-295-5510. www.uline.com

# Manufacturer

## Mauser Packaging Solutions, 1515 W. 22nd St., Suite 1100, Oak Brook, IL 60523, Tel: 800-527-2267.

# Reference Part Number(s)

## Supplier model number: S-10757BLU

## Supplier part description: Plastic Drum – 55 Gallon, Closed Top, Blue

# Specification

## Capacity: 55 Gallon

## UN Rating: 1H1/Y1.9/100

## Dimensions (Total Height x Diameter): 34.25” x 23.25”

## Thickness: 2.2mm

## Color: Blue

## Material (Lid & Drum): High density polyethylene (BPA free)

# Certificates

## A Certificate of Conformance (CoC) from the manufacturer is required for each batch/lot number of product.

# Receiving Inspection

## Ensure there is no visible signs of damage to the container.

## Review the manufacturer CoC and packing slip and verify order documentation for quantity and part number match.