SOURCE CONTROL SPECIFICATION

Part Number: C.SLQ001

Only the item described in this source control to meet the specification listed herein is approved by SILQ.  A substitute item shall not be used without prior approval.

# Purpose

## This document provides the specification for Silq’s Suspension.

# Manufacturer

## Silq Technologies, Inc., 323 Sunny Isles Blvd., 7th Floor, Sunny Isles Beach, FL 33160, Tel: (424) 309-8523, Contact email: info@silq.tech, website: www.Silq.tech

# Reference Part Number(s)

## Manufacturer part number: C.SLQ001

# General Information

## Handling:  Wear goggles and gloves when handling the material. Keep in a closed container until ready to use. The dispersion may settle to the bottom of the container during storage. Use an overhead mixer to redisperse the material before use.

## Storage: Keep the chemical solution in a dry place at ambient temperature until ready to use.

# Specification

## Description: The C.SLQ001 Suspension solution is a water-based coating solution for polymeric and elastomeric surfaces. The solution contains a three-component methacrylate copolymer, polymerized via free radical polymerization from polysulfobetaine methacrylate, perfluorophenylazide methacrylate, and methacrylic acid. The copolymer stricture and mol ratios of each component of the polymer is shown below:

## The material is dispersed at 1 w/v% in deionized water.

## Materials Specification:

### Appearance (color)*: Opaque white suspension

### Appearance (form)*: Inviscid liquid

### Residue on Evaporation*: 0.5% – 1.5%

### pH*: 5-8

## Packaging: The material is packaged in HDPE bottles or drums

## Performance capabilities: When irradiated with UV-C light, it binds to surfaces to resist adhesion of organic material, increases hydrophilicity, and reduces tackiness. The coating can also serve as a primer layer for overcoating to improve bond strength and durability. Upon irradiation with UV-C light, a thin layer of material is deposited on the surface of the substrate or device. In some cases, the surface treatment is very thin and can only be detected through contact angle measurements. In other cases, the surface treatment can be visible to the naked eye. Several factors modify the deposition of the surface treatment such as: UV irradiation time, irradiation intensity, chemical concentration, and pH.

# Certificates

## A Certificate of Analysis (CoA) from the manufacturer is required for each batch/lot number of product.

# Receiving Inspection

## Ensure there is no visible signs of damage to the product primary container.

## Review the manufacturer CoA and packing slip and verify order documentation for quantity and part number match.

## Review the manufacturer CoA and verify the product properties listed above with an asterisk (*) match material specifications or are within required ranges.

### If the solution looks yellow in color, dispose of it immediately. Consistent with dispersions, the solids may settle to the bottom of the container during storage.